TABLE III.

*A Table exhibiting the different descriptions of Timber, of good quality, to be used in the Timbering, Outside and Inside Planking, of Ships, as the same mill be applicable to the several terms of Years appointed for Ships to remain on the First Description of the First Class. From Lloyd's Register of British and Foreign Shipping for* 1840-41.

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Parts of a Vend.** | **First Class. Twelve Years.** | | **First Class. Ten Yean.** | **First Class. Nine Years.** | **First Class. Eight Years.** | | **First Class. Seven Years.** | | | | **First Class. Six Years.** | **First Class. Five Years.** | **First class. Four Years.** | **Paru of a Vessel.** |
| **Floors** |  |  | **Live oak and red cedar** |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | **alternately**  **Adriatic")**  **. Spanish )oak**  **French )**  **South American or** | **. Other foreign white oak and red cedar** |  |  | **English ash**  **Sound second-hand**  **English or African oak or teak** | | | | **English beech Larch Hackmatack** | **Baltic fir** |  |  |
| **First futtocks** |  |  | **New South Wales hard wood**  **Live oak and red cedar alternately**  **Adriatic Ί** | **Other foreign white** |  |  | **Other foreign oak above light water-** | | | | **English ash** | **Red pine**  **Black birch**  **Foreign elm or ash Hardwood of good quality** | **• White spruce** |  |
|  |  | **'English'! African >oak Live *J***  **East India teak** | **. Spanish J-oak**  **French J** | **oak below the light water.mark** |  |  | **mark**  **Sound second-hand** | | | | **. Larch**  **Hackmatack** |  |  |  |
|  |  | **South American hard wood** | **Red cedar** |  |  |  | **English or African oak or teak** | | |  |  |  |  |
| **Second futtocks** |  | **Morung saul**  **Greenheart** |  | **Adriatic )** |  |  |  |  |  |  | **Γ.rrh** |  | **Elm** |  |
|  | **.Morra** |  | **Spanish .'•oak** |  |  |  |  |  |  | **Hackmatack** |  |  |
|  |  |  | **Live oak and red cedar** | **French *J***  **South American hard wood**  **Red cedar** |  |  |  |  |  |  | **■ Sound second hand English or African oak, or teak** | **Baltic fir** | **Black birch white spruce** | **Frame** |
|  |  |  | **alternately** | **Adriatic Ί** |  |  |  |  |  |  |  | **Red pine** | **Yellow pine Elm**  **- Ash** |  |
| **Third futtocks and top-timbers** |  |  |  | **Spanish >oak**  **French J**  **South American or** |  |  |  |  |  |  | **Hackmatack**  **Pitch-pine** |  |  |
|  |  |  |  | **New South Wales** |  |  |  |  |  |  | **English or African** |  | **Black birch** |  |
|  |  |  |  | **hard wood Red cedar** |  |  | **Other oak** | | | **foreign white** | **oak~, or teak** |  | **white spιuce** |  |
| **Stem and stem poet** |  | **r English·)**  **African Soak** |  | **Adriatic Ί** |  |  |  |  |  |  | **Hackmatack Larch** |  | **Black birch** |  |
|  |  |  | **Spanish toak French 1** |  |  |  |  |  |  |  |  |  |  |
| **Transoms, knight-heads, hawse tun-** |  | **Live 1**  **East India teak** |  | **South American hard wood**  **Red cedar** |  |  |  |  |  |  | **Larch**  **Hackmatack Sound second-hand** | **Baltic fir Red pine** | **Yellow pine**  **Elm**  **Ash** |  |
| **berg, apron** |  |  |  |  |  |  |  |  |  |  | **English or African** | **Black birch** |  |
|  |  |  |  |  |  |  |  |  |  | **oak, or teak** |  | **White spruce** |  |
| **Main keelson** |  |  | **Adriatic Ί**  **Spanish >oak**  **French )**  **South American, nr** |  |  |  |  |  |  |  | **Keltic fir** |  |  |  |
|  |  | **English ) African Soak** | **Other foreign white oak** |  |  | **Pitch-pine** | | | | **Red pine American rock elm** | **Ash** |  |  |
|  |  | **New South Wales hard wood** |  |  |  |  |  |  |  | **Hackmatack** |  | **Yellow pine** | **Keelson** |
| **•** |  | **Live 1** | **Red cedar** |  |  |  |  |  |  |  |  |  | **Beams** |
|  |  | **East India teak** | **Adriatic Ί » S** |  |  |  |  |  |  |  |  |  | **Black birch** | **- Hooks** |
| **Beams, hooks, and** |  | **Morung saul** | **Spanish >oak French )** |  |  |  |  |  |  |  | **Baltic fir** |  | **VV bite spruce** | **Knees** |
|  | **Greenheart** |  |  |  | **Fitch-** | | | **pine** | **Red pine** | **Foreign elm** |  |
| **knees** |  | **Moira** | **South American hard** |  | **Other foreign white** | | **Larch** | | | **Hackmatack** |  |  |
|  |  | **wood** |  | **oak** |  | **Knees** | | | **of fir, pitch-** | **Sound second-hand** | **Ash** |  |  |
|  |  |  | **New South Wales do.** |  |  |  |  | **pine, or spruce** | | | **English or African** |  |  |  |
|  |  |  | **and red cedar for beams only** |  |  |  |  |  |  |  | **oak, or teak** |  |  |  |
| **Keel to first futtock heads** | **English Ί** | |  |  |  |  |  |  |  |  |  |  |  |
|  | **African >oak**  **Live i East India teak**  **Red cedar** | | **Pitch pine** | **∏nltir fir** |  |  |  |  |  |  |  | **Yellow pine** |  |  |
|  | **Foreign white oak**  **fi‰)-** | | **Larch Black birch** | **Red pine** |  |  |  |  |  |  |  | **White spruce** |  |  |
|  | **Beech**  **South American or** | |  |  |  |  |  |  |  |  | **Hackmatack** |  |  |  |
|  |  | **any hard wood** |  |  | **\*** |  |  |  |  |  |  |  |  |